## Slide 1
Advances in Scanning Probe Microscopy
Eric I. Altman1 and Udo D. Schwarz1,2
1Department of Chemical & Environmental Engineering
2Department of Mechanical Engineering & Materials Science
https://seas.yale.edu/faculty-research/faculty-directory/eric-altman
https://www.eng.yale.edu/nanomechanics/

## Slide 2
Atomic Resolution Surface Imaging and Characterization
Altman Lab:
UHV STM in Surface Analysis System with Small Growth Chamber.
300 – 900 K, up to 3 images/sec
Focus on imaging chemical and physical processes on surfaces as they occur.
Schwarz Lab:
UHV Low T Combined STM/AFM.
» 4 K, interrogate the same atom for hours.
Focus on chemical and physical property characterization with high spatial and energy resolution.
Canal Level – Malone Engineering Center

## Slide 3
Developing the Ideal Surface Microscopy/Spectroscopy Tool
In a single experiment:
Image atoms
Identify types of atoms
Determine the chemical states of atoms
Characterize individual chemical bonds
Measure molecule-surface interaction energies
Measure molecule-molecule interaction energies
Characterize overlap of electronic states responsible for the interactions
Probe specific atoms on demand
Assemble structures with atomic precision and measure the energetics of each step

## Slide 4
Mapping Molecule-Surface Interactions – 3D-AFM

## Slide 5
3D AFM – Surface Oxide Layer on Cu(100)
Potential Energy Landscape
Average energy subtracted; color scale: -9.4 meV (dark blue) to 9.4 meV (dark red)

## Slide 6
Multi-Dimensional Imaging – Distinguishing Types of Atoms
Potential Energy ® Tunneling Current
The tunneling current maxima are between the rows of maxima in the potential energy image.
The current image reflects the rows of Cu atoms between the O rows.

## Slide 7
Characterizing Overlap of Electronic States Responsible for Chemical Interactions
3D-STM
V
z–V spectra equivalent to ln(I)–V curves.
Amorphous 2D SiO2 -2.75 - -0.75 V

## Slide 8
Measuring Molecule-Molecule Interactions

## Slide 9
Measuring Molecule-Molecule Interactions
Data for C6H5I
Potential Energy
Vertical Force
Lateral Force

## Slide 10
Contribution to Yale Community
Unique surface imaging and combined surface analysis capabilities.
Expertise in long-term, high-precision measurements.
Expertise in frequency-based methods.
Critical Needs
Access to rapid electronics development, prototyping, etc.
Assistance with more rapidly developing data acquisition and analysis software.
Development of methods for rapid image and data analysis- potentially a large amount of data in the detailed tip trajectory.
How Can Yale Instrumentation Initiative Help?
Meet above critical needs.
Development of a user high-resolution SPM facility to work with the Yale community on a broad range of problems.

## Slide 11
Department of Energy Basic Energy Sciences
National Science Foundation Chemistry and Materials Research Divisions
Petroleum Research Fund
Yale Center for Research on Interface Structure and Phenomena